SECTION 07920 - JOINT SEALANTS

GENERAL

RELATED DOCUMENTS

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

SUMMARY

This Section includes sealants for the following:

Exterior joints in vertical surfaces and nontraffic horizontal surfaces.

Exterior joints in horizontal traffic surfaces.

Interior joints in vertical surfaces and horizontal nontraffic surfaces.

Exterior joints in sheet metal flashing and trim.

Exterior joints around metal door and window frames.

See Section 02752 "Concrete Paving Joint Sealants" (Article 2.04) for pavement sealant joints installed in Portland cement paving and between Portland cement and asphalt paving.

See Section 03300 or 03310 “Cast in Place Concrete” for Semi-Rigid Polyurea Joint Filler for interior concrete slabs.

See Division 7 Section Aluminum Cornice and Section Metal Wall Panels for Sealant.

See Section 07241  “Exterior Insulation and Finishing Systems” for EIFS joint sealant.

See Division 8 Section "Glazing" for glazing sealants.

SUBMITTALS

The General Contractor and the Sub-Contractor shall execute the provided Conformance Submittal for the product(s) specified.

The General Contractor and the Sub-Contractor shall utilize ONLY the products as noted in this specification.  NO SUBSTITUTIONS ALLOWED.

All submittals are to be made on Site / Folio (www.sitefolio.net).

QUALITY ASSURANCE

Sealant Compatibility and Adhesion Testing:  Use sealant manufacturer's standard test methods to determine whether priming and other specific joint preparation techniques are required to obtain rapid, optimum adhesion of joint sealants to joint substrates.

Preconstruction Field-Adhesion Testing:  Before installing elastomeric sealants, field test their adhesion to joint substrates using test method indicated in Part 3 "Field Quality Control" Article.

Mockups:  Before installing joint sealants, apply elastomeric sealants to demonstrate aesthetic effects and qualities of materials and execution.

Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

WARRANTY

Special Installer's Warranty: Written warranty in which Installer agrees to repair or replace elastomeric joint sealants that do not meet requirements specified in this Section or fail in adhesion within specified warranty period two years from date of Final Acceptance.

PRODUCTS

MANUFACTURERS

In other Part 2 articles where subparagraph titles below introduce lists, the following requirements apply for product selection:

Products:  Subject to compliance with requirements, provide one of the products specified.

MATERIALS, GENERAL

Compatibility:  Provide joint sealants, backings, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by sealant manufacturer based on testing and field experience.

Colors of Exposed Joint Sealants shall match adjacent finish unless otherwise indicated on drawings.

  - ELASTOMERIC JOINT SEALANTS

- A.	Silicone Sealant: (Metal Door and Window Frames, Gutters, Coping, and Miscellaneous Flashing Sealant)

Products:

Dow Corning; 795.

GE Silicone, SilPruf.

Tremco Spectrem 2

- B.	Single-Component Nonsag Urethane Sealant:

- For vertical masonry control joints, provide the following:

            - Products:

Sonneborn Building Products Div., ChemRex Inc.; NP 1.

Tremco; Vulkem 116.

Sika Corporation; Sikaflex - 1a.

Type and Grade:  S (single component) and NS (nonsag).

Class:   25.

Exposure:  Use T (traffic) and NT (nontraffic).

Substrates:  Uses M, G, A, and, as applicable to joint substrates indicated, O.

Silicon Sealant:  (Precast Tilt-up & Precast Walls)

Products.

Dow Corning, 790

BE Silicone, SilPruf.

Tremco Spectrem 3 or 4 TS.

Tremco Dymoni FC (at fire-rated precast).

For pre-finished precast walls, sealant color to match precast.

Urethane Sealant:

Exterior - concrete paving joints, horizontal traffic surfaces, and general use not specified otherwise.

Products:

Eucolid, Eucolastic I or II

Bostik, “Chem-Calk 950”.

Sonneborn, “SL-1”.

Tremco, Vulkem 45

Type and Grade S (single component) and NS (nonsag).

Class 25

Exposure:   T (traffic).

Substrate:   O

      - FAST SETTING SEMI-RIGID POLYUREA FLOOR JOINT FILLER – Refer to Section 03300 or 03310 “Cast in Place Concrete” for Semi-Rigid Polyurea Joint Filler for interior concrete slabs.

JOINT-SEALANT BACKING

General:  Provide sealant backings of material and type that are nonstaining; are compatible with joint substrates, sealants, primers, and other joint fillers; and are approved for applications indicated by sealant manufacturer based on field experience and laboratory testing.

Cylindrical Sealant Backings:  ASTM C 1330, of size and density to control sealant depth and otherwise contribute to producing optimum sealant performance:

Type:  C (closed-cell material with a surface skin).

Bond-Breaker Tape:  Polyethylene tape or other plastic tape recommended by sealant manufacturer for preventing sealant from adhering to rigid, inflexible joint-filler materials or joint surfaces at back of joint where such adhesion would result in sealant failure.  Provide self-adhesive tape where applicable.

MISCELLANEOUS MATERIALS

Primer:  Material recommended by joint sealant manufacturer where required for adhesion of sealant to joint substrates indicated, as determined from preconstruction joint-sealant-substrate tests and field tests.

Cleaners for Nonporous Surfaces:  Chemical cleaners acceptable to manufacturers of sealants and sealant backing materials, free of oily residues or other substances capable of staining or harming joint substrates and adjacent nonporous surfaces in any way, and formulated to promote optimum adhesion of sealants with joint substrates.

Masking Tape: Non-staining, nonabsorbent material compatible with joint sealants and surfaces adjacent to joints.

EXECUTION

INSTALLATION OF JOINT SEALANTS

Contractor performing work must be one the Sealant Manufacturer’s Approved Applicators.

Surface Cleaning of Joints: Clean out joints immediately before installing joint sealants.

Remove foreign material from joint substrates that could interfere with adhesion of joint sealant.

Clean porous joint substrate surfaces by brushing, grinding, blast cleaning, mechanical abrading, or a combination of these methods to produce a clean, sound substrate capable of developing optimum bond with joint sealants.  Remove loose particles remaining from above cleaning operations by vacuuming or blowing out joints with oil-free compressed air.

Remove laitance and form-release agents from concrete.

Clean nonporous surfaces with chemical cleaners or other means that do not stain, harm substrates, or leave residues that could interfere with adhesion of joint sealants.

All surfaces to be caulked shall be clean and dry.

Joint Priming:  Prime joint substrates where recommended in writing by joint sealant manufacturer, based on preconstruction joint-sealant-substrate tests or prior experience.  Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

Coordinate with Section 07241 EIFS.  Sealant is to be applied to the base coat only and not the finish coat.

Masking Tape:  Use masking tape where required to prevent contact of sealant with adjoining surfaces that otherwise would be permanently stained or damaged by such contact or by cleaning methods required to remove sealant smears.  Remove tape immediately after tooling without disturbing joint seal.

Sealant Installation:  Comply with recommendations in ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions indicated.

Install sealant backings to support sealants during application and at position required to produce optimum sealant movement capability.

Do not leave gaps between ends of sealant backings.

Do not stretch, twist, puncture, or tear sealant backings.

Remove absorbent sealant backings that have become wet before sealant application and replace them with dry materials.

Install bond-breaker tape behind sealants where sealant backings are not used between sealants and back of joints.

Place sealants so they directly contact and fully wet joint substrates.

Completely fill recesses provided for each joint configuration.

Produce uniform, cross-sectional shapes and depths that allow optimum sealant movement capability.

All deep cracks shall be filled to within 1/2 inch of the surface with an appropriate back-up material and caulked with a caulking gun.  Caulking beads shall be smooth and straight.

Caulk around all door and storefront openings and where noted on the drawings.

Masonry, Tilt-up, or Precast control joints shall be caulked with a high-quality paintable urethane caulk.  Control depth of caulk at 3/8 inch to 1/2 inch with a continuous closed-cell rod.

Tooling of Nonsag Sealants:  Immediately after sealant application and before skinning or curing begins, tool sealants to form smooth, uniform beads, to eliminate air pockets, and to ensure contact and adhesion of sealant with sides of joint.

Remove excess sealants from surfaces adjacent to joint.

Use tooling agents that are approved by sealant manufacturer and that do not discolor sealants or adjacent surfaces.

Joint Configuration:  Concave joint configuration per Figure 5A in ASTM C 1193, unless otherwise indicated.

INSTALLATION OF SEMI-RIGID POLYUREA JOINT FILLER– Refer to Section 03300 or 03310 “Cast in Place Concrete” for Semi-Rigid Polyurea Joint Filler for interior concrete slabs.

END OF SECTION 07920

# CONFORMANCE SUBMITTAL

# Section 07920 – Joint Sealants

Lowe’s of ____________________________________________________________________________

(City, State)

General Contractor:	________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

Sub-Contractor:		________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

The following product has been selected (check one box) for use in this project from the list of acceptable products specified:

Silicone Sealant: (Hollow Metal Door Frames, Gutters, Coping, and Miscellaneous Flashing)

Dow Corning; 795

GE Silicone, SilPruf

Tremco Spectrem 2

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

General Contractor:	________________________________________________________________

(Signature of the Authorized Agent of the General Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the General Contractor)

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

Sub-Contractor:		________________________________________________________________

(Signature of the Authorized Agent of the Sub-Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the Sub-Contractor)

# CONFORMANCE SUBMITTAL

# Section 07920 – Joint Sealants

Lowe’s of ____________________________________________________________________________

(City, State)

General Contractor:	________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

Sub-Contractor:		________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

The following product has been selected (check one box) for use in this project from the list of acceptable products specified:

Single – Component Nonsag Urethane Sealant:

Sonneborn Building Products Div., Chemrex Inc.; NPI.

Tremco; Vulkem 116.

Silka Corporation; Silkaflex-1a

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

General Contractor:	________________________________________________________________

(Signature of the Authorized Agent of the General Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the General Contractor)

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

Sub-Contractor:		________________________________________________________________

(Signature of the Authorized Agent of the Sub-Contractor)

________________________________________________________________

# (Print Name of the Authorized Agent of the General Contractor)
CONFORMANCE SUBMITTAL

# Section 07920 – Joint Sealants

Lowe’s of ____________________________________________________________________________

(City, State)

General Contractor:	________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

Sub-Contractor:		________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

The following product has been selected (check one box) for use in this project from the list of acceptable products specified:

Urethane Sealant:

Bostik, “Chem-Calk 950”

Sonneborn, “SL-1”

Tremco, Vulkem 45

Tremco,  Vulkem 45 SSL

Euclid, Eucolastic I

Euclid, Eucolastic II

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

General Contractor:	________________________________________________________________

(Signature of the Authorized Agent of the General Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the General Contractor)

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

Sub-Contractor:		________________________________________________________________

(Signature of the Authorized Agent of the Sub-Contractor)

________________________________________________________________

# (Print Name of the Authorized Agent of the General Contractors)

# CONFORMANCE SUBMITTAL

# Section 07920 – Joint Sealants

Lowe’s of ____________________________________________________________________________

(City, State)

General Contractor:	________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

Sub-Contractor:		________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

The following product has been selected (check one box) for use in this project from the list of acceptable products specified:

Silicone, SilPruf:

Dow Corning, 790”

GE Silicone, SilPruf”

Spectrem 3

Tremco Spectrem 4 TS

Tremco Dymonic FC

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

General Contractor:	________________________________________________________________

(Signature of the Authorized Agent of the General Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the General Contractor)

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

Sub-Contractor:		________________________________________________________________

(Signature of the Authorized Agent of the Sub-Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the General Contractors)