SECTION 09300 – CERAMIC TILE

GENERAL

RELATED DOCUMENTS

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

SUMMARY

This Section includes the following:

Porcelain floor tile.

Porcelain Wall tile

REFERENCES

American national Standards Institute (ANSI):

A108.5 - Installation of Ceramic tile with Dry-Set Portland Cement or Latex-Portland Cement.

A108.10 - Installation of Grout in Tilework.

A108.13 - Installation of Membranes for Thin-Set Ceramic Tile.

A118.4 - Latex-Portland Cement Mortar.

A118.6 - Ceramic Tile Grouts.

A137.1 - Ceramic Tile

American Society for Testing and Materials (ASTM):

#### C 136 - Sieve Analysis of Fine and Coarse Aggregates.

#### C 144 - Aggregate for Masonry Mortar.

#### C 150 - Portland Cement.

#### C 627 – Robinson Floor Test for Tile Service Level.

#### C 1028 - Static Coefficient of Friction of Ceramic Tile and Other Like Surfaces by the Horizontal Dynamometer Pull-Meter Method.

TCA Handbook for Ceramic tile Installation by Tile Council of America, latest edition.

SUBMITTALS

The General Contractor and the Sub-Contractor shall execute the provided Conformance Submittal for the product(s) specified.

The General Contractor and the Sub-Contractor shall utilize ONLY the products as noted in this specification.  NO SUBSTITUTIONS ALLOWED.

PROJECT CONDITIONS

Maintain a temperature of not less than 72 deg F or more than 95 deg F in spaces to receive floor tile for at least 48 hours before installation, during installation, and for at least 48 hours after installation, unless manufacturer's written recommendations specify longer time periods.

After post installation period, maintain a temperature of not less than 72 deg F or more than 95 deg F.

Install floor tile after other finishing operations, including painting, have been completed.

All concrete surfaces that are to receive ceramic tile shall be inspected by the installing contractor, if found unsatisfactory the work of laying the ceramic tile shall not commence until the defective surfaces have been made satisfactory.  Beginning work constitutes an acceptance of the base concrete flooring.

QUALITY ASSURANCE

The work covered by this Section of the specifications includes the furnishing of all labor, equipment, appliances, materials and the performing of all operations in connection with the laying, installing and finishing of all ceramic tile in strict accordance with the applicable drawings, schedules, and the approved samples and color selection.

SINGLE SOURCE RESPONSIBILITY:

Tile:  Minimum 5 years experience in manufacture of tile products.

Setting Materials:  Minimum 10 years experience in manufacture of setting and grout materials specified.

INSTALLER QUALIFICATIONS:

Specializing in tile work having minimum of 5 years successful documented experience with work comparable to that required for this Project.

CERTIFICATIONS:

Submit "Master Grade Certificate" for each tile type in accordance with requirements of ANSI A137.1.

Submit manufacturer's certifications that mortars, adhesives, and grouts are suitable for intended use.

Conform to ANSI – Recommended Standard Specifications for Ceramic Tile – A137.1.

Conform to TCA Ceramic Tile: The Installation Handbook.

WARRANTY

### A.	Special Project Warranty:  Submit a written warranty, executed by the Contractor, Installer, and Manufacturer, agreeing to repair or replace tile that fails in materials or workmanship within the specified warranty period.

Warranty Period: 2 years after date of Final Acceptance.

PRODUCTS

- Contact the local Crossville Distributor or Crossville National Accounts Deptartment @ 931-484-2110 for Lowe’s National Account pricing on all Crossville, Inc. products.

GLAZED PORCELAIN FLOOR TILE

Products:  Subject to compliance with requirements, provide the following:

Crossville Glazed Porcelain Floor Tile, 12”x 24” AV295 Magma

Substitutions not permitted.

WALL TILES

Products: Subject to compliance with requirements, provide the following:

Crossville Glazed Porcelain Wall Tile, 12”x 24” AV292 Caldera

Provide 4” x 12” bullnosed tile at locations where tile edge is exposed AV292 Caldera (i.e. vertical edge of exposed wall tile).

Provide 6” x 12” Crossville Glazed Porcelain Universal Cove Base, AV295 Magma

MORTAR

Latex Portland Cement Thin Bed Adhesive Mortar

Dry set mortar to be weather, frost, shock resistant meeting the following physical requirements:

Compressive strength						5000 psi (34.5 MPa) Min. (ANSI A118.4)

Bond strength							500 psi (3.5 Mpa) Min. (ANSI A118.4)

Water absorption							4% Max. (ANSI A118.6)

Smoke & Flame contribution factors		0 (ASTM E84 – Modified)

Acceptable Products

Hydroment, Single-Flex F.S. (#973 Gray) thin-set mortar with admixture #425 Multi-Purpose Acrylic Latex.

Laticrete, premium floor ‘n’ wall thin set mortar gauged with mortar admix #3701.

GROUT

Chemical-Resistant Epoxy Grout for Floor Tile:

Description: Stain-proof, chemical resistant 100% solids epoxy with temperature resistance and comply with ANSI A118.3.

Acceptable Products:

Laticrete Easy Poxy, color 45 Raven

Hydroment EzPoxy, color H142 French Gray

Mapei Kerapoxy, color 47 Charcoal

### Sanded Latex-Modified Grout for Wall Tile:

#### Description:  Latex-modified, factory blended, mildew resistant, sanded, grout consisting of portland cement and additives; comply with ANSI A118.6.

#### Latex Additive:  Type as recommended by latex mortar manufacturer.

#### Acceptable Products:

##### Laticrete Ceramic Tile grout (sanded), color 45 Raven

##### Hydroment, Ceramic Tile grout (sanded), color H142 French Gray

##### Mapei Keracolor S Ceramic Tile Grout (sanded) color 47 Charcoal

INSTALLATION ACCESSORIES

Trowelable Leveling and Patching Compounds:  Latex-modified, portland cement-based or blended hydraulic cement-based formulation provided or approved by flooring manufacturer for applications indicated.

Tile Edge:  Provide edge strip Schlüter-Reno Ramp (AERP-125-B90).  Schlüter Systems 1-800-472-4588.

Edge strip is to be provided in one continuous piece from edge to edge of opening.

EXECUTION

INSTALLATION

Concrete Subfloors:  Verify that concrete slabs comply with ASTM F 710 and the following:

Slab substrates are dry and free of curing compounds, sealers, hardeners, and other materials that may interfere with adhesive bond.  Determine adhesion and dryness characteristics by performing bond and moisture tests recommended by flooring manufacturer.

Tile Installation, General:

Install tile materials in accordance with ANSI A137.1, other referenced ANSI and TCA specifications, and TCA "Handbook for Ceramic Tile Installation", except for more stringent requirements of manufacturer or these Specifications.

Cut and fit tile tight to protrusions and vertical interruptions and treat with a compatible sealant as specified in Section 07920 Joint Sealants.  Form corners and bases neatly.  Install tile edge in accordance with manufacturer recommendations.

Work tile joints uniform in width, subject to variance in tolerance allowed in tile size.  Make joint watertight, without voids, cracks, excess mortar, or grout.

Prepare surface, fit, set, bond, grout and clean in accordance with applicable requirements of ANSI standards and Tile Council of America.

Floors - Dry-set:  TCA F113

Walls - Dry-set on Masonry:  TCA W202.

Do not seal tile or grout.

MORTAR

Thin bed method:  Apply mortar with notched trowel to work installation materials into good contact with tile substrate.  Select trowel notch size per tile selected.  Spread only as much mortar as can be covered in 20-30 minutes or while mortar surface is still wet and tacky.  When installing large tiles, spread (back-butter) mortar onto back of each tile in addition to troweling materials over tile substrate.  Beat each piece into mortar with a beating block or rubber mallet to insure full bedding and flatness.  Allow installation to set until firm.  Clean excess mortar from tile surface.

GROUTING

Allow tiles to set a minimum of 48 hours before grouting.

If bonding materials are rapid setting, follow manufacturer’s recommendations.

Install in accordance with grout manufacturer's recommendations and ANSI A108.10.

Pack ¼” wide joints full and free before mortar takes initial set.

Clean excess grout from surface with wet cheesecloth as work progresses.  Do not use hydrosponges.

Install sealant to match grout in vertical wall joints at interior corners.

CLEANING

Clean excess mortar from surface with water as work progresses.  Perform cleaning while mortar is fresh and before it hardens on surfaces.

Sponge and wash tile diagonally across joints.  Polish with clean dry cloth

END OF SECTION 09300

This Page Left Intentionally Blank

# CONFORMANCE SUBMITTAL

# Section 09300 – Ceramic Tile

Lowe’s of ____________________________________________________________________________

(City, State)

General Contractor:	________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

Sub-Contractor:		________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

The following product has been selected (check one box) for use in this project from the list of acceptable products specified:

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

Porcelain Floor Tile, Grout and Transition Strip:

Crossville, Inc. AV295 MAGMA.

Laticrete Easy Poxy 45 Raven

Hydroment EzPoxy,, color H142 French Gray.

Mapei Kerapoxy, color 47 Charcoal

Schlüter-Reno-Ramp (AERP-125-B90)

General Contractor:	________________________________________________________________

(Signature of the Authorized Agent of the General Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the General Contractor)

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

Sub-Contractor:		________________________________________________________________

(Signature of the Authorized Agent of the Sub-Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the Sub-Contractor)

# CONFORMANCE SUBMITTAL

# Section 09300 – Ceramic Tile

Lowe’s of ____________________________________________________________________________

(City, State)

General Contractor:	________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

Sub-Contractor:		________________________________________________________________

(Company Name)

________________________________________________________________

(Address, Phone Number)

The following product has been selected (check one box) for use in this project from the list of acceptable products specified:

Porcelain Wall Tile and Grout:

Crossville, Inc. AV1292 CALDERA

Laticrete Ceramic Tile Grout (sanded), color 45 Raven

Hydroment , Ceramic Tile Grout (sanded), color H142 French Gray.

Mapei Keracolor S Ceramic Tile Grout (sanded) color 447 Charcoal

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

General Contractor:	________________________________________________________________

(Signature of the Authorized Agent of the General Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the General Contractor)

I represent to Lowe’s that the product selected will be installed in compliance with the applicable codes for the authorities having jurisdiction and in accordance with the project specification.  If noncompliance is discovered the General Contractor shall make or cause to be made all necessary corrections to meet the applicable codes and specifications.  Immediately or as directed by Lowe’s the work shall be completed without additional cost to the Lowe’s and / or the contract.

Sub-Contractor:		________________________________________________________________

(Signature of the Authorized Agent of the Sub-Contractor)

________________________________________________________________

(Print Name of the Authorized Agent of the Sub-Contractor)