SECTION 09911 – PAINTING

- GENERAL

  - RELATED DOCUMENTS

    - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

    - See Section 7 Joint Sealants.

  - SUMMARY

    - This Section includes surface preparation and field painting of exposed exterior and interior items and surfaces.

    - The work to be done by the painting contractor shall include the furnishing of all material, labor, tools and equipment required to complete the painting and finishing of the building as specified.  Painting contract does not include shop coats.  This contractor shall caulk around all exterior door and window frames in such a manner as to make them absolutely air tight.

  - SUBMITTALS

    - Product Data:  For each product indicated.

    - Samples:  For each type of finish-coat material and color chips indicated.

    - Exterior wall coating submittal form.

  - QUALITY ASSURANCE

    - General contractor shall schedule and coordinate a pre-paint application meeting, virtual or on-site, at least one (2) weeks prior to commencing work on this section.  Notify Owner at least three (3) weeks in advance of meeting date.  Required attendees will be Painting Contractor, General Contractor, Coating Manufacturer’s Technical Representative and Owner.   The agenda shall include:

      - Apply block filler/surfacer and top coat to a section of split-face wall (minimum 4’-0” x 6’-0” in size) in accordance with specifications and to the satisfaction of all attendees.  Record project conditions and coverage site (for general information only).  Upon approval, further work may proceed and this sample shall establish standards (but not coverage rates), by which the work will be judged, and shall remain intact until the work is accepted.

      - Review contract drawings, coating manufacturer’s application requirements, status of coordinating work, availability and adequacy of materials, proposed schedule and application procedures.

      - Record discussion including agreement/disagreement on matters of significance and furnish copies to each participant.  If substantial disagreements exist, determine how these will be resolved and set date to reconvene meeting as appropriate.

      - General Contractor to upload attendee list and meeting notes to sitefolio for records of meeting.

    - Benchmark Samples (Mockups): Provide a full-coat benchmark finish sample for each type of coating and substrate required.  Comply with procedures specified in PDCA P5.

      - Wall Surfaces:  Provide samples on at least 100 sq. ft. (9 sq. m).

      - Small Areas and Items:  Owner will designate items or areas required.

      - Final approval of colors will be from benchmark samples.

    - Inspections:

      - The Coating Manufacturer’s Technical Representative shall be on-site or provide verification of product and conditions, at the beginning of installations for both the exterior wall base and finish coat applications to insure the following:

        - The correct colors are on hand for use.

        - The correct types of coatings are on hand for use.

        - The wall conditions are reviewed with the applicator for manufacturer’s compliance.

        - The coatings are being applied per manufacturer’s recommendations.

      - The manufacturer’s representative must fill out the “Exterior Wall Coating Submittal Form”, found in this section, and turn it in to the General Contractor upon completion of work.

    - Graffiti Solution System by PROSOCO – (Al Morris, National Sales Manager (800) 255-4255, Fax: (800) 877-2700.  Sure Klean Blok-Guard® & Graffiti Control II.), shall be applied only by licensed, certified applicators that are under contract with the manufacturer and that are recommended by the manufacturer for the application of the Graffiti Solution System.  Applicators shall provide certificate signed and dated by the manufacturer prior to bid.

  - PROJECT CONDITIONS

    - Store materials not in use in tightly covered containers in a well-ventilated area at a minimum ambient temperature of 45 deg F (7 deg C).  Maintain storage containers in a clean condition, free of foreign materials and residue.

    - Apply paints only when temperatures of surfaces to be painted and surrounding air are between 45 and 95 deg F (7 and 35 deg C).

    - Do not apply paint in snow, rain, fog, or mist; or when relative humidity exceeds 85 percent; or at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

- PRODUCTS

  - MANUFACTURERS

    - Products:  Subject to compliance with requirements, provide one of the products listed in other Part 2 articles.

    - Paint Manufacturers' Names:  Shortened versions (shown in parentheses) of the following manufacturers' names are used in other Part 2 articles:

      - Sto Corp (Sto)- contact: Mark Hight (615) 981-4744

      - PPG Architectural Finishes, Inc. (PPG) – contact:  Rick Garlin (317) 318-5800

      - Textured Coatings of America (TCA) for exterior tilt-up concrete only – contact:  Richard Barnes 800-454-0340; Simon Reynolds, VP Commercial Sales (954) 205-5117

      - Sherwin Williams (SW) – contact: Paul Faudree, Director of Sales (216) 288-5498 email: paul.faudree@sherwin.com

  - COLORS

    - Exterior Colors:

      - Lowe’s Light Beige, Lowe’s Medium Beige, Blue and Red are to be produced in accordance with each manufacturer’s approved color formulation.  See drawings for locations.  Contact the manufacturer’s national account representative for these formulas.

    - Interior Colors:

      - See drawings for locations, colors and manufacturers.

  - COATINGS

    - Exterior Masonry Waterproofing System Manufacturer:  for colors Lowe’s, Medium Beige, Light Beige or different colors as indicated on drawings. Tinting is not allowed.

      - Sto Corp:

        - #520 Sto Prime Block Surfacer HP (do not tint), 1coat, 14-16 wet mils as block fill (more coats may be required for highly porous, rough, or irregular surfaces), 1 coat 4-6 wet mils as a primer

- White: NA13-0009

        - #217 Sto Coat Lotusan, 2 coats (5-7 wet mils per coat)

- Lowe’s Light Beige: NA12-0069

- Lowe’s Medium Beige: NA12-0067

- Lowe’s White: NA13-0009

    - Exterior Masonry Waterproofing System Manufacturer for accent colors Lowe’s Blue or Red or different accent colors as indicated on drawings.

      - Sto Corp:

        - #520 Sto Prime Block Surfacer HP (do not tint), 1 coat, 14-16 wet mils as block fill (more coats may be required for highly porous, rough, or irregular surfaces), 1 coat 4-6 wet mils as a primer #520 Sto Prime Block Surfacer HP needed only on masonry; Not required if over new or existing EIFS.

1)   White: NA13-0009

        - #648 Sto Coat Acryl Plus, 2 coats (8-10 wet mils per coat)

- Lowe’s Blue: NA12-0070

- Lowe’s Red: NA12-0071

        - #512 Sto Clear Coat Sealer, 2 coats (2-3 wet mils per coat)

    - Interior Exposed Roof Structure:

      - Exposed roof structure in Main building to be painted using the dryfall / dry fog application interior metal including decking, structural steel, joists framing, piping, etc.

        - PPG: Speedhide Super Tech Alkyd  Dry-Fog # 6-151 XI, Eggshell or LEED compliant Version # 6-724XI Speedhide Super-Tech  Acrylic Eggshell Dry Fog.

        - SW: Super Save-Lite Hi Tech Dryfall – B48 series, Eg-Shel or LEED compliant Pro Industrial Waterbased Dryfall, Eg-Shel – B42 series.

    - Exterior Precast Concrete

      - Sto Corp:

        - At smooth locations indicated on drawings:

          - Exterior Primer: #805 Sto Hot Prime, 1 coat (4-6 wet mils)

          - Exterior Smooth Surface Finish: #217 Sto Coat Lotusan, 2 coats (5-7 wet mils per coat)

        - At textured location indicated on drawings:

          - Exterior Primer: #805 Sto Hot Prime, 1 coat (4-6 wet mils)

          - Textured Surface Finish: #659 Sto Coat Texture Medium (applied at 50-75 SF per gal)

      - Textured Coatings of America – TEX-COTE

        - At smooth locations indicated on drawings:

          - TEX-COTE XL-70 Primer at 350-400 SF per Gallon

          - TEX-COTE 300 Smooth Coatings at approximately 50 +/- 5 SF per gallon.

        - At textured location indicated on drawings:

          - TEX-COTE XL-70 Primer at 350-400 SF per Gallon

          - TEX-COTE 300 Textured Coatings at approximately 50 +/- 5 SF per gallon.

      - Textured Coatings of America–TEX-COTE (If requested by Construction Project Manager)

        - At smooth locations indicated on drawings:

          - TEX-COTE XL-70 Primer at 350-400 SF per Gallon.

          - TEX-COTE 70 Smooth Coatings at approximately 50 +/- 5 SF per gallon.

        - At textured location indicated on drawings:

          - TEX-COTE XL-70 Primer at 350-400 SF per Gallon.

          - TEX-COTE 70 Textured Coatings at approximately 50 +/- 5 SF per gallon.

      - Sherwin-Williams:

        - At smooth locations indicated on drawings:

          - Exterior Primer: Loxon Concrete and Masonry Primer, LX02 Series (5.3 – 8 wet mils per coat)

          - Exterior Smooth Surface Finish: Loxon Self Cleaning Acrylic Coating, LX13  Series, 2 coats (5-7 wet mils per coat)

        - At textured location indicated on drawings:

          - Exterior Primer: Loxon Concrete and Masonry Primer, LX02 Series (5.3 – 8 wet mils per coat)

          - Textured Surface Finish: ConFlex UltraCrete Acrylic Textured Coating, CF17 Series (applied at 50-80 SF per gallon).

        - At textured location indicated on drawings: (if requested by Construction Project Manager)

          - Textured Surface Finish: ConFlex Flexible Concrete Waterproofer Textured, CF15 Series, 2 coats (10-20 wet mils per coat).

    - Interior Masonry and Precast Concrete System Manufacturers

      - PPG Industries:

        - 1 Coat Speedhide 6-15XI Latex Block Filler (at masonry walls only).

        - 2 Coats Pro EV 12-110XI Interior Flat

      - SW:

        - 1 coat Preprite Latex Block Filler – B25 series (at masonry walls only).

        - 2 Coats ProMar 400 Zero Flat Latex – B30 series

    - Interior Drywall System Manufacturers (Three coats per manufacturer’s recommendations).

      - PPG:

        - 1 coat Pro EV 12-900XI Latex Primer Sealer

        - 2 coats Pro EV 12-510XI Interior Semi-Gloss Latex

      - SW:

        - 1 coat ProMar 400 Zero Latex Primer – B28 series

        - 2 coats ProMar 400 Zero Semi-Gloss – B31 series

    - Traffic Coatings:

        - H&C Concrete Sealer – Solid Color Solvent Based – note: sealers and curing agents MUST be removed prior to application. Refer to product data page for prep and applications recommendations.

    - Exterior Ferrous Metal (including all exposed steel roof decking, structural steel, joists, framing, piping, etc.)

      - PPG

        - Primer: PPG: 4160 Multi-Prime Tank & Structural Primer (use for areas with rust, pitting or exposed metal rust. Complete prime on metal within 10 miles of coastal areas.

        - Finish: PPG:   Pitt Tech 90-812 EDF Series -Acrylic Semi-Gloss Dry Fog.

      - STO

        - Primer: Sto Corp: 81825-StoPrime® DTM (for use on areas with rust on carbon steel, galvanized steel, aluminum, and other properly prepared metal surfaces.) Apply at 5.0-7.5 mils WFT to achieve 2.5-4.0 mils DFT.)

        - Finish: Sto Corp: 81863-StoColor® DTM Gloss or 81824-StoColor® DTM Semi-Gloss. (for use on prepared metal surfaces) Apply at 4.5–6.0 mils WFT to achieve 1.5- 2.1 mils DFT per coat.

      - Sherwin-Williams

        - Primer: SW Macropoxy 646 FC Semi-Gloss, B58 Series (use for areas with rust, pitting or exposed metal rust. Complete prime on metal within 10 miles of coastal areas).

        - Finish: SW SprayLastic Exterior Semi-Gloss Dryfall, B42 Series

    - Exterior Ferrous Metal (excluding fencing systems – see Sections 02822 and 02825).

      - PPG:   Pitt Tech Plus EP 90-1710 Series.   Acrylic Satin DTM.

      - Sto Corp: 81863-StoColor® DTM Gloss or 81824-StoColor® DTM Semi-Gloss. (for use on prepared metal surfaces) Apply at 4.5–6.0 mils WFT to achieve 1.5- 2.1 mils DFT per coat.

      - Sherwin-Williams: SW Pro Industrial DTM Acrylic Eg-shel, B66 Series

    - Interior Ferrous Metal:

      - PPG:  Pitt Tech EP 90-1710 Series.  Interior/Exterior High Performance High Gloss DTM Industrial Enamel or PPG Pitt Tech EP 90-1510.  Interior/Exterior High Performance Satin DTM Industrial Enamel.

      - Sto Corp: 81863-StoColor® DTM Gloss or 81824-StoColor® DTM Semi-Gloss. (for use on prepared metal surfaces) Apply at 4.5–6.0 mils WFT to achieve 1.5- 2.1 mils DFT per coat.

      - Sherwin-Williams: Pro Industrial DTM Acrylic Gloss, B66 Series.  Pro Industrial DTM Acrylic Eg-shel, B66 Series

      - .

    - Graffiti Solution System Manufacturer: (if indicated on drawings for use on Pre-Colored Masonry and Brick only)

      - PROSOCO – Al Morris, National Sales Manager (800) 255-4255, Fax: (800877-2700.

        - Sure Klean ® Weather Seal Blok-Guard® & Graffiti Control II. (for use on Pre-colored masonry and Brick)

        - Defacer Eraser® Sacrificial Coating SC-1 (for use on Painted Masonry)

      - General Paint – GSS Graffiti Solution System – Gord Clark – Arch Account Manager 416-991-8499

    - Exterior Wood Stain:

      - Samuel Cabot – Semi-Transparent Stain.

      - PPG – Flood Pro Series Semi-Transparent Acrylic/Oil Stain

      - SW – Woodscapes Polyurethane Semi-Transparent Stain – A15 series.

      - Color to later selection from manufacturer’s standard range of colors.

    - Interior Epoxy System:

      - PPG:

        - 1 coat Speedhide 6-15XI Latex Block Filler for block or 1 coat Pro EV 12-900XI Latex Primer Sealer for drywall.

        - 2 coats Pitt-Glaze W.B.1Precatalized Semi-Gloss Acrylic Epoxy (16-1510 series).

      - SW:

        - 1 coat Preprite latex Block Filler (B25 Series) for block or 1 coat ProMar 400 Zero Latex Primer (B28 Series) for drywall.

        - 2 coats Industrial Pre-Catalyzed Epoxy Semi Gloss – K46 series.

  - PAINT MATERIALS, GENERAL

    - Material Compatibility:  Provide block fillers, primers, and finish-coat materials that are compatible with one another and with the substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.

    - Material Quality:  Provide manufacturer's best-quality paint material of the various coating types specified that are factory formulated and recommended by manufacturer for application indicated.  Paint-material containers not displaying manufacturer's product identification will not be acceptable.

    - Graffiti Solution System Manufacturer:  (if indicated on drawings for use on Pre-Colored Masonry and Brick only)

    - Colors:  As indicated on drawings.

  - PREPARATORY COATS

    - The contractor shall be wholly responsible for the finish of this work, and shall not commence any part of it until surface is in proper condition.

    - All knots or sappy spots shall be given one coat of shellac before painting.  All necessary puttying of nail holes, cracks and blemishes shall be done after priming coat has become hard and dry and before second coat is applied.  All greasy or oily metal surfaces shall be cleaned with solvent before applying any materials.   All scale or rust shall be removed by scraping or wire brushing.

    - Any unprimed steel, galvanized steel, or Galvalume steel shall be prepared by solvent methods in accordance with paint manufacturer’s recommendations.

- EXECUTION

  - APPLICATION

    - The following requirements shall be met in addition to those of the manufacturer:

      - Block wall Surfaces:

        - Apply block filler/surfacer with airless spray followed by a double back roll to insure proper fill and appearance.  Filler/surfacer coat shall be virtually pin-hole free.  Areas exhibiting more than ten (10) pin-holes per block shall be recoated.

        - Top coat shall be applied with airless spray followed by a double back roll to insure proper build and appearance.  All “running” shall be eliminated by back rolling.  Top coat shall be virtually pin-hole free.  Areas exhibiting more than ten (10) pin-holes per block shall be recoated.  Roller strokes shall be indiscernible.

      - Contractor shall be responsible for a thorough and complete application as required by these specifications regardless of coverage rates which may be suggested by the manufacturer.

    - Comply with procedures specified in Painting and Decorating Contractors of America (PDCA) P4  “responsibilities for inspection and acceptance of surfaces to be painted.”

    - All work shall be performed in a workmanlike manner by skilled mechanics.  All materials shall be properly applied and shall be free from runs or sags.  No paint, varnish or enamel shall be applied until preceding coat is thoroughly dry and hard.

    - Unless otherwise specified, exterior oil paints shall be allowed to dry at least 48 hours between coats; interior paints at least 24 hours between coats.  Enamel and varnish shall be allowed to dry at least 48 hours between coats and shall be sanded lightly between coats with #00 sandpaper and dusted before succeeding coat is applied.  After applying paste wood fillers, excess shall be carefully and neatly cleaned from surface by rubbing across grain.  All nail holes shall be filled with putty or other approved filler, tinted to match finish.

    - Coordination of Work:  Review other Sections in which primers are provided to ensure compatibility of the total system for various substrates.  On request, furnish information on characteristics of finish materials to ensure use of compatible primers.

    - Remove hardware and hardware accessories, plates, machined surfaces, lighting fixtures, and similar items already installed that are not to be painted.  If removal is impractical or impossible because of size or weight of the item, provide surface-applied protection before surface preparation and painting.

      - After completing painting operations in each space or area, reinstall items removed using workers skilled in the trades involved.

    - Surface Preparation:  Clean and prepare surfaces to be painted according to manufacturer's written instructions for each particular substrate condition and as specified.

      - Provide barrier coats over incompatible primers or remove and re-prime.

      - Cementitious Materials:  Remove efflorescence, chalk, dust, dirt, grease, oils, and release agents.  Roughen as required to remove glaze.  If hardeners or sealers have been used to improve curing, use mechanical methods of surface preparation.

      - Wood:  Clean surfaces of dirt, oil, and other foreign substances with scrapers, mineral spirits, and sandpaper, as required.  Sand surfaces exposed to view smooth and dust off.

        - Scrape and clean small, dry, seasoned knots, and apply a thin coat of white shellac or other recommended knot sealer before applying primer.  After priming, fill holes and imperfections in finish surfaces with putty or plastic wood filler.  Sand smooth when dried.

        - Prime, stain, or seal wood to be painted immediately on delivery.  Prime edges, ends, faces, undersides, and back sides of wood, including cabinets, counters, cases, and paneling.

        - If transparent finish is required, back prime with spar varnish.

        - Back prime paneling on interior partitions where masonry, plaster, or other wet wall construction occurs on back side.

        - Seal tops, bottoms, and cutouts of unprimed wood doors with a heavy coat of varnish or sealer immediately on delivery.

        - Paint both sides and edges of plywood backboards for electrical equipment before installing backboards and mounting equipment on them.

      - Ferrous Metals:  Clean galvanized ferrous-metal surfaces that have not been shop coated or rusting; remove oil, grease, dirt, loose mill scale, rust and other foreign substances.  Use solvent or mechanical cleaning methods that comply with the Society for Protective Coating’s (SSPC) recommendations.

        - Blast steel surfaces clean as recommended by paint system manufacturer and according to SSPC-SP 6/NACE No. 3.

        - Treat bare and sandblasted or pickled clean metal with a metal treatment wash coat before priming.

        - Touch up bare areas and shop-applied prime coats that have been damaged or exhibit rust.  Wire-brush, clean with solvents recommended by paint manufacturer, and touch up with same primer as the shop coat.

        - All unprimed exposed metal shall be given a prime coat of Alkyd Rust Inhibitive metal primer and two top coats. Use grey 94-269 by PPG Industries.  Metal arriving at the job with shop prime coat applied shall be carefully sanded and all bare spots re-primed before painting.  Interior hollow metal door/frames, exposed sprinkler lines and other interior exposed metal surfaces shall be painted as indicated on drawings.

      - Galvanized Surfaces:  Clean galvanized surfaces with nonpetroleum-based solvents so surface is free of oil and surface contaminants.  Remove pretreatment from galvanized sheet metal fabricated from coil stock by mechanical methods.

      - Gypsum Wallboard:  All gypsum wallboard shall be given a minimum of two coats of paint.  Additional coats may be required to achieve acceptable coverage.  See drawings for paint types and colors.

    - Material Preparation:

      - Maintain containers used in mixing and applying paint in a clean condition, free of foreign materials and residue.

      - Stir material before application to produce a mixture of uniform density.  Stir as required during application.  Do not stir surface film into material.  If necessary, remove surface film and strain material before using.

    - Exposed Surfaces:  Include areas visible when permanent or built-in fixtures, grilles, convector covers, covers for finned-tube radiation, and similar components are in place.  Extend coatings in these areas, as required, to maintain system integrity and provide desired protection.

      - Paint surfaces behind movable equipment and furniture the same as similar exposed surfaces.  Before final installation of equipment, paint surfaces behind permanently fixed equipment or furniture with prime coat only.

      - Finish exterior doors on tops, bottoms, and side edges the same as exterior faces.

      - Finish interior of wall and base cabinets and similar field-finished casework to match exterior.

    - Sand lightly between each succeeding enamel and varnish coat.

    - Scheduling Painting:  Apply first coat to surfaces that have been cleaned, pretreated, or otherwise prepared for painting as soon as practicable after preparation and before subsequent surface deterioration.

      - Omit primer over metal surfaces that have been shop primed and touchup painted.

      - If undercoats, stains, or other conditions show through final coat of paint, apply additional coats until paint film is of uniform finish, color, and appearance.

    - Application Procedures:  Apply paints and coatings by brush, roller, spray, or other applicators according to manufacturer's written instructions.

    - Minimum Coating Thickness:  Apply paint materials no thinner than manufacturer's recommended spreading rate.  Provide total dry film thickness of the entire system as recommended by manufacturer. Provide average wet mil thickness for all walls taken at a minimum of 4 evenly spaced locations per wall length and height.

    - Mechanical and Electrical Work:  Painting of mechanical and electrical work is limited to items exposed in equipment rooms and occupied spaces.

    - Block Fillers:  Apply block fillers to concrete masonry block at a rate to ensure complete coverage with pores filled.

    - Prime Coats:  Before applying finish coats, apply a prime coat, as recommended by manufacturer, to material that is required to be painted or finished and that has not been prime coated by others.  Recoat primed and sealed surfaces where evidence of suction spots or unsealed areas in first coat appears, to ensure a finish coat with no burn-through or other defects due to insufficient sealing.

    - Pigmented (Opaque) Finishes:  Completely cover surfaces as necessary to provide a smooth, opaque surface of uniform finish, color, appearance, and coverage.  Cloudiness, spotting, holidays, laps, brush marks, runs, sags, ropiness, or other surface imperfections will not be acceptable.

    - Transparent (Clear) Finishes:  Use multiple coats to produce a glass-smooth surface film of even luster.  Provide a finish free of laps, runs, cloudiness, color irregularity, brush marks, orange peel, nail holes, or other surface imperfections.

  - CLEANING AND PROTECTING

    - At the end of each workday, remove empty cans, rags, rubbish, and other discarded paint materials from Project site.

    - Protect work of other trades, whether being painted or not, against damage from painting.  Correct damage by cleaning, repairing or replacing, and repainting, as reviewed by the Owner.

    - Provide "Wet Paint" signs to protect newly painted finishes.  After completing painting operations, remove temporary protective wrappings provided by others to protect their work.

      - After work of other trades is complete, touch up and restore damaged or defaced painted surfaces.  Comply with procedures specified in PDCA P1.

  - EXTERIOR PAINT SCHEDULE (also see drawings)

    - Concrete Unit Masonry:

      - Surface Preparation:    All interior and exterior CMU shall be free from dirt, loose or excess mortar, and thoroughly dry before painting.  Painting of CMU may proceed 30 days after installation under normal drying conditions.  Refer to manufacturer’s recommendations for surface curing and dryness requirements prior to application of exterior masonry waterproofing system.  All CMU shall be free of visible efflorescence prior to painting.   See Division 4 for efflorescence removal.

    - Ferrous Metal (including all exposed metal under Garden Center roof and Customer Loading Canopy roof):

      - Direct to Metal (DTM) Acrylic Finish:  Two finish coats over a rust-inhibitive primer.

        - Primer:  Exterior ferrous-metal primer (not required on shop-primed items).

        - Finish Coats:  Exterior semi-gloss DTM acrylic enamel.

    - Zinc-Coated Metal:

      - Direct to Metal (DTM) Acrylic Finish:  Two finish coats over a galvanized coat and metal primer.

        - Primer:  Exterior galvanized metal primer.

        - Finish Coats:  Exterior semi-gloss DTM acrylic enamel.

  - EGRESS PATH IN GARDEN CENTER AND STAGING AREA ON CONCRETE (and other interior locations, as indicated on drawings):

    - Paint unobstructed path, as indicated on drawings.

    - Paint shall be applied in two (2) coats to a clean, dry surface, per manufacturer’s recommendations.

  - EXTERIOR MASONRY WATERPROOFING SYSTEM (AS INDICATED ON DRAWINGS)

    - General Description:  Furnish all materials and labor for complete and through application of waterproofing system as described herein to all above-grade exterior masonry surfaces.

  - DRYFALL / DRY FOG / DRY DROP APPLICATION

    - Surfaces to be finished must be clean, dry and free of dirt, oils, or other contaminates.

    - Application shall be conventional spray gun or airless spray pump.   Do not apply when atmospheric or surface temperature is below 50 degrees F.

    - Contractor shall insure all areas to be painted are covered and touched up as required.  All surfaces surrounding painted areas shall be fully protected from accidental spraying.

    - Contractor shall clean up paint residue on walls and floors prior to end of working day.

  - SURFACES NOT TO BE PAINTED

    - Acoustical tiles, concrete, vinyl floor tile, aluminum, U.L. equipment and stainless steel metal equipment shall receive no paint.  All paint spots shall be removed from the above surfaces.

  - ANTI-GRAFFITI COATING (if indicated on drawings)

    - Products:

      - PROSOCO Al Morris, National Sales Manager (800) 255-4255, Fax: (800) 877-2700

        - Sure Klean ® Weather Seal Blok-Guard ® & Graffiti Control II

        - Defacer Eraser® Sacrificial Coating SC-1

      - Graffiti Solution System manufactured by American Polymer Corporation.  Contact:   American Polymer Corporation (801) 255-9505 or by fax (801) 255-7123.

    - Deliver materials to the job site in the manufacturer’s original, new, unopened packages, and containers bearing manufacturer’s name and label.

    - Store materials not in use in tightly covered containers in a well-ventilated area at a minimum ambient temperature of 45 deg F. (7 deg C).  Maintain containers used in storage in a clean condition, free of foreign materials and residue.

    - Apply coatings only when the temperature of surfaces to be coated and surrounding air temperatures are between 45 deg F (7 deg C) and 95 deg F (35 deg C).

    - Do not apply coatings in snow, rain, fog, or mist; when the relative humidity exceeds 85 percent; when temperature is less than 50 deg F (3 deg C) above the dew point; or to damp or wet surfaces.  (Exception:  low temperature systems may be used upon approval by Lowe’s project manager as directed in accordance with manufacturer’s recommendations.)

      - Allow wet surfaces to dry thoroughly and attain the temperature and conditions specified before proceeding with or continuing the coating operation.

    - Examine substrates and conditions under which coatings will be applied for compliance with requirements on applying coatings.  Surfaces to receive coatings must be thoroughly dry before coatings are applied.

      - Do not proceed with coating application until unsatisfactory conditions have been corrected.

      - Start of application will be construed as the applicator’s acceptance of surfaces within that particular area.

    - Cleaning:   Before applying coatings or other surface treatments, clean the substrates of substances that could impair bond of the various coatings.  Remove oil and grease prior to cleaning.  Schedule cleaning and coating application so dust and other contaminates from the cleaning process will not fall on wet, newly coated surfaces.

    - Cementitious surfaces: Prepare concrete, concrete masonry block, cement plaster, and similar surfaces to receive special coatings.  Remove efflorescence, chalk, dust, dirt, grease, oils and release agents.  Roughen, as required, to remove glaze.  If hardeners or sealers have been used to improve concrete curing, use mechanical methods to prepare surfaces.

      - Use abrasive blast-cleaning methods if recommended by the coating system manufacturer.

      - Determine alkalinity and moisture content of surfaces to be coated by performing appropriate tests.  If surfaces are sufficiently alkaline to cause the finish coats to blister and burn, correct this condition before application.  Do not apply coatings over surfaces where the moisture content exceeds that permitted in the manufacturer’s printed directions.

    - Material Preparation:  Carefully mix and prepare materials according to the coating manufacturer’s directions.

      - Maintain containers used in mixing and application of coatings according to the manufacturer’s directions.

      - Stir materials before applying to produce mixture of uniform density; stir as required during application.  Do not stir surface film into the material.  Remove film and, if necessary, strain the coating material before using.

    - General:   Apply special coatings by brush, roller, spray, squeegee, or other applicators according to the manufacturer’s directions.   Use brushes best suited for the material being applied.  Use rollers of carpet, velvet back, or high-pile sheep’s wool as recommended by the manufacturer for the material and texture required.

      - Do not apply coatings over dirt, rust, scale, grease, moisture, scuffed surfaces, or conditions detrimental to forming a durable coating film.

    - Minimum Coating Thickness:  Apply each material no thinner than the manufacturer’s recommended spreading rate.  Provide total dry film thickness of the entire system as recommended by the manufacturer.

    - Cleanup:  At the end of each work day, remove rubbish, empty cans, rags and other discarded materials from the site.

    - Protect work of other trades, whether being coated or not, against damage from coating operation.  Correct damage by cleaning, repairing, replacing, and recoating, as acceptable to the owner.  Leave in an undamaged condition.

  - Warranty/Guarantee

    - Contractor shall guarantee that all labor and materials provided shall be of first quality, in full compliance with the requirements of the Contract Documents, and free from defect for a period of one (1) year from date of Final Acceptance of the work.

    - Contractor shall obtain from the manufacturer of the exterior wall coating system a written warranty which warrants to the Building Owner for a period of five (10) years (and/or specific product warranty extensions for 10 years as applicable) from the date Final Acceptance of the work that the exterior coating system shall be free of defects in manufacture and the surface coating will not sustain peeling, cracking or blistering, excessive chalking, excessive chipping, excessive fading (per defined standards for specific products), nor allow water penetration, under ordinary wear.  This warranty shall provide for sufficient materials (and labor as applicable to specific products) to replace products which fail to meet these requirements.

    - Contractor to upload warranty document from coatings manufacturer to sitefolio as part of the close out documents.

  - CLEANING

    - The contractor shall be responsible for the condition of building to his charge.  He shall protect adjacent work and materials from soiling or damage as well as his own.  Upon completion of all painting work, the contractor shall remove all paint from door knobs, floors, counter tops and other areas not requiring paint.  Touch up all scuff marks and make the whole project in first class condition.  Remove all equipment, debris and surplus materials.

END OF SECTION 09911

|  | EXTERIOR WALL COATING SUBMITTAL FORM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Project: |  |  |  |  |  |  |  |  | City: |  |  |  |  |  |  |  |
| General Contractor: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Paint Manufacturer: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Paint Mfr. Rep. Name: |  |  |  |  |  |  |  |  | Phone # |  |  |  |  |  |  |  |
| Paint Contractor: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Paint Contractor's Address: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Paint Contr. Contact Name: |  |  |  |  |  |  |  |  | Phone # |  |  |  |  |  |  |  |
| SURFACE PREPARATION (prior to application) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Type of Surface to be coated (Block, Pre-Cast Conc., Tilt-Up Conc., etc.) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Signature of approval accepting surface for application: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  | (Paint Contractor) |  |  |  |  |  | Date |  |
| PRIMER/BLOCK FILLER (do not tint) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Product to be applied: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Area to be covered (s.f.): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Gallons to be used: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Product applied per specification: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  | (Paint Contractor) |  |  |  |  |  | Date |  |
| Approved specified product supplied: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  | (Manufacturer) |  |  |  |  |  | Date |  |
| Date Application Started: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Weather Conditions: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expected 24 hr. High Temp.: |  |  |  |  |  |  |  |  | Expected 24 hr. Low Temp.: |  |  |  |  |  |  |  |
| FINISH COATING SYSTEM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Product to be applied: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color: |  |  |  |  | Area of coverage (s.f.): |  |  |  |  |  |  | No. coats: |  |  |  |  |
|  |  |  |  |  | Gallons to be used: |  |  |  |  |  |  | (per coat) |  |  |  |  |
|  |  |  |  |  | Wet Mil Thickness: |  |  |  |  |  |  |  |  |  |  |  |
| Color: |  |  |  |  | Area of coverage (s.f.): |  |  |  |  |  |  | No. coats: |  |  |  |  |
|  |  |  |  |  | Gallons to be used: |  |  |  |  |  |  | (per coat) |  |  |  |  |
|  |  |  |  |  | Wet Mil Thickness: |  |  |  |  |  |  |  |  |  |  |  |
| Color: |  |  |  |  | Area of coverage (s.f.): |  |  |  |  |  |  | No. coats: |  |  |  |  |
|  |  |  |  |  | Gallons to be used: |  |  |  |  |  |  | (per coat) |  |  |  |  |
|  |  |  |  |  | Wet Mil Thickness: |  |  |  |  |  |  |  |  |  |  |  |
| Weather Conditions: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expected 24 hr. High Temp.: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Wet Mil Thickness Average at Test Locations(4 locations per wall): |  |  |  |  |  |  |  | Expected 24 hr. Low Temp.: |  |  |  |  |  |  |  |  |  |